## Slide 1: RCS power system and magnets Seminar Series for the National Lab Muon Accelerator Study Group
1 CERN , 2 UNR –Còrdoba (AR) , 3 KIT –Karlsruhe (DE), 4 UNIBO – Bologna (IT), 5 TUD-Darmstadt (DE), 6 UNILAVAL-Quebec (CA)
F. Boattini1, G. Brauchli2, M. Gast3, D. Fazioli4,D. Moll5, M. Breschi4, D. Aguglia1, P. Viarouge6

## Slide 2: Fast Ramping Magnets
Transient problem
Main components:
  Laminated iron core: nonlinear, hysteretic
  Conductors: skin- & proximity effects
    Cooling system?
  Beam pipe: induced currents
Different operation modes:
  RCS 2,3,4: zero mean operation
  RCS 1 with DC offset
  Duty cycle ~ 1%
Focus on RCS1 and RCS2
IMCC Interim report, 2024

## Slide 3: Numerical Modeling - Maxwell
Developed transient electrodynamic FEM framework
Nonlinear constitutive relationship
  Saturation
  Hysteresis (Energy-based model)
  Eddy currents
Detailed loss calculation in time and space
Maxwell‘s equations:
  Magnetic Gauss:
  Faraday-Lenz:
  Ampère:
Ohm‘s law:
10.1109/TMAG.2025.3639643

## Slide 4: Insights of FEM Analysis
In-house software allows in depth analysis
of local behavior in time and space
Runtime ~ O(30min)
Loss density of single pulse (J/m³)
First cycle differs due to
wrong initial state
Peak excitation current: 50kAt (12.5kA per bar)

## Slide 5: Losses per Period
Copper loss: 75.93 J/m
Titanium loss: 16.46 J/m
Iron loss: 25.11 J/m
Copper loss: 69.21 J/m
Titanium loss: 16.43 J/m
Iron loss: 22.89 J/m
Copper loss: 48.24 J/m
Titanium loss: 16.31 J/m
Iron loss: 22.69 J/m
Study of different duty cycles. Goal: compare to frequency domain methods.
Losses given per cycle!

## Slide 6: Frequency- Domain Loss Evaluation Method
Objective: Balance accuracy& computational speed for loss estimation in pulsed steady-state regimes with Time-harmonic FEA for efficient iterative optimal design
Fourier decomposition of periodic current pulse on
Time-harmonic FEA for each harmonic 𝑛=0 - 7
Sum harmonic contributions to compute steady-state losses on
Sum Compute average steady-state losses on
Real & Reconstructed Signal
(𝑛=0 - 7 ) on
Steady-state obtained on on with Transient FEA
Courtesy Prof. Philippe Viarouge

## Slide 7: Cross-Validation Between Simplified Time-Harmonic and High-Fidelity Transient FEA Model
Benchmark: Transient FEA with magnetic saturation & dynamic hysteresis
Simplified Time-Harmonic FEA (linear, frequency-domain) faster to compute steady-state Joule & magnetic losses
Loss evaluation with both methods
  for steady-state operation on
  Valid despite simplified assumptions (steady-state, linear)

## Slide 8: Equivalent Circuit & Nonlinear Dynamic Modeling
Time-Harmonic FEA results allow identification of an equivalent circuit with the same frequency response, usable in time-domain simulation
  3 R-L cells fitted by least-squares to match impedance frequency response obtained by Time-harmonic FEA & to model induced eddy current in bars
Nonlinear extension of the dynamic model:
  obtained via saturated magnetostatic FEA using magnetic material B(H)
  Analytical fit → nonlinear inductance inserted into equivalent circuit
Nonlinear hybrid equivalent circuit:

## Slide 9: Cross-Validation Between Simplified Time-Harmonic and High-Fidelity Transient FEA Model
Dynamic Validation of the Equivalent Circuit Using Transient FEA
Validation scenario:
  Nonlinear hybrid equivalent circuit model driven by pulsed power converter in Simulink
  Simulated input magnet voltage applied to Voltage supplied full Transient FEA model
Agreement on Current waveform reproduction
Transient FEA
Voltage
Current Pulse
Simulink
Transient FEA
SPS-Simulink

## Slide 10: Field Quality Analysis
Field quality evaluated on several 5 mm reference circles. (All in vacuum chamber)
Multipole coefficients [T] as function of time and position
Air gap and beam pipe with
10µm Titanium coating
20mm
50mm
30mm
lower at peaks
due to saturation

## Slide 11: Beam Pipe Affecting Field Quality
Without beam pipe:
With beam pipe:
Unwanted
multipole coefficients
are larger on average.
Similar peak values.
Symmetry in time
is lost.

## Slide 12: Relative Multipole Coefficients
Relative multipole coefficients:
Requirement: 10 Units on 10 mm reference circle
  Green region
Strong quadrupole and sextupole coefficients: Shim design recommended / ongoing
Without beam pipe:
With beam pipe:

## Slide 13: RCS2 Dipole Analysis FEM + Circuit
Analysis of Magnet FEM Model + Circuit
Vs‘=3.13kV/m C‘=1.17mFm
Rs C=25ms
Current not ideally triangular

## Slide 14: RCS2 Dipole Analysis Striped Beam Pipe Coat
Analysis of Magnet FEM Model + Circuit
Beam pipe coating: 10µm Titanium
  Scenario : One connected layer
  Scenario : Four separate stripes
Considerable losses
Can be reduced by striped coat