## Slide 1: Solenoids for the Muon Collider
K. Badgley
March 23, 2026

## Slide 2: Solenoid Locations

## Slide 3: Target, Capture, Decay
Evolution of MAP design to IMCC design
  Resistive hybrid to full HTS
  Increased solenoids spacing for support structure
  Increase bore shielding
  Simplify power supply-all coils at the same current
Solenoids covered in Luca Bottura’s talk
https://indico.muoncollider.us/event/26/

## Slide 4: Target, Capture, Decay
Coil beyond state of the art
Solenoids covered in Luca Bottura’s talk
https://indico.muoncollider.us/event/26/

## Slide 5: Initial cooling*
Helical FOFO (HFOFO)
Alternating polarity, tilted solenoids (periodic rotations in x and z, pitch and roll) to generate rotating dipole
30 periods with 6 solenoids per period
Modest magnetic fields, current density <100 A/mm2
Can be achieved with current technology
Example of one period
D. Neuffer, 2016
C. Riggall, 2025

## Slide 6: 6D Cooling Schemes Considered
Guggenheim helix
Ring
Rectilinear
Not pictured- Helical

## Slide 7: 6D Cooling
Solenoids with superimposed dipole
  MAP used titled solenoids
  IMCC solenoids with separate dipoles
Two lattices: pre-merge (A), post-merge (B)
  A 4 stages
  B 10 stages (IMCC variant with shorter 8 stage)
Each stage has ~100 cells
At least three current designs, more in progress
Large forces (tens of MN) due to alternating field direction and nearby coils
A1 cell
B1 cell
R. Zhu, 2025
B4 cell
B6 cell

## Slide 8: 6D Cooling
Fields ~sinusoidal
Axis field from 2-17 T
Bore radius 70-600 mm
Over 25 unique solenoids
Two branches, one for each sign
One charge branch requires ~3,000 magnets, so a total of ~6,000 solenoids!

## Slide 9: Final Cooling
At least 3 lattice designs at present, depending on 6D cooling choice
  IMCC- beam after 6D cooling stage 8 and after stage 10
MAP design 10 alternating high field solenoids separated by 10 lower field solenoids
Required field up to ~43 T
Current density ~632 A/mm2
https://arxiv.org/pdf/2510.27437
MAP
*B. Bordini et al., "Conceptual Design of a ReBCO Non/Metal-Insulated Ultra-High Field Solenoid for the Muon Collider," in IEEE Transactions on Applied Superconductivity, 2024
60 mm
730 mm

## Slide 10: Beyond State-of-the-Art
Chart: Inner Diameter of SC Coils (m)
| 3.4000000000000002E-2 | 3.4000000000000002E-2 | 7.4999999999999997E-2 | 7.4999999999999997E-2 | 7.4999999999999997E-2 | 0.11 | 0.7 | 1.1000000000000001 | 0.6 | 0.3 | 1.8 | 0.6 | 2.6 | 0.53 | 0.88 | 0.9 | 0.65 | 1 | 1 | 1 | 1 | 0.68 | 6
HTS (T) | 32 | 28.2 | 25.8
HTS Dev (T) | 40
LTS (T) | 23.5 | 21.1 | 14 | 11.3 | 13 | 12 | 9 | 7 | 10.5 | 9.4 | 9.4 | 7 | 3 | 1.5 | 11.75 | 11.75 | 3.8
LTS Dev (T) | 15 | 11
State-of-the-Art
MagLab 40 T
MC 6D Cooling
MC Target, decay, & capture 20 K
MC Final Cooling
Field vs Bore of Superconducting Solenoids
LTS = Low Temperature Superconductors (NbTi, Nb3Sn)
HTS = High Temperature Superconductors (REBCo, Bi-2223, Bi-2212)
Plot from Mark Bird with minor modifications

## Slide 12: REBCO-Structure
Rare-earth Barium Copper Oxide
  yttrium, lanthanum, samarium, neodymium, gadolinium and europium
Fabrication
  Physical vapor deposition- pulsed laser, sputtering, molecular beam epitaxy,…
  Chemical vapor deposition- Metal-organic chemical vapor deposition, plasma enhanced
  Atomic layer deposition
a-b plane of crystal structure ~ along plane of tape
Critical current density is highly anisotropic, depends on B field orientation to crystal structure
  Design winding to minimize perpendicular field?
www.superpower-inc.com
a
b
c
J Jaroszynski et al 2022 Supercond. Sci. Technol. 35 095009

## Slide 13: REBCO- Fabrication and Winding
Formed as wide tape and mechanically or laser slit to desired width, leads to non-uniformity in thickness at the edges
Non-uniform thickness creates voids in winding, voids lead to kinks and non-uniform turn-to-turn resistance
M. Small 2021
J. Bang 2025 Little Big Coil
300 turns
R. Unterrainer 2025

## Slide 14: REBCO-Mechanical Limits
Longitudinal driven by plastic deformation of substrate causing cracking in REBCO
Transverse compression driven by stress concentration
Maeda et al. 2014
Several images taken from G. Vernassa’s talk Performance Limitations of UHF REBCO Solenoids
M. Sugano et al 2005 Supercond. Sci. Technol. 18 S344
Loading direction
Grains of Hastelloy
Limits bend radius

## Slide 15: REBCO-Mechanical Limits
Layered structure vulnerable to delamination
Delamination driven by local defects
  Cracks, delamination nucleation sites, inclusions…
Need non-destructive method of characterizing tapes
Several images taken from G. Vernassa’s talk Performance Limitations of UHF REBCO Solenoids
Slit edge side
1 μm
Al2O3
Hastelloy® C-276
Y2O3
EuBCO
Ag
MgO
Delamination
2.5 μm
Hastelloy® C-276
EuBCO
Al2O3
Y2O3
MgO
Ag
Mixed crack./delam.
Slit edge side
Cracks at slit edges
Stress concentration at crystallites
Adapted from P. Gao et al., Supercond. 2023

## Slide 16: Screening Currents – Little Big Coil Program
12 NI pancakes in 31 T background field
Stress from screening current caused plastic deformation
Orientation of slit edge appeared to play a role
  Result of crystal tilt and non-uniform Jc instead
J. Bang, 2025
M. Wang, 2019

## Slide 17: REBCO – Additional R&D Areas
Non-uniform critical current across width of tape
  Use multiple tapes in parallel
Quench protection
  Slow normal zone propagation ~cm/s
  Non-insulated vs insulated
Low resistance splice method
Radiation damage
Need to match simulation to experiments
  Couple electromagnetic and mechanical simulations
  Screening currents change inductance
Test larger coils
  Cooling, powering, quench protection
…
YateStar measurement of critical current at 77K of SuperPower tape
Paul Yu
T. Mulder

## Slide 18: Coil Test Facilities
Commercial Facilities
  Commonwealth Fusion, GA ITER central solenoid,…
Refurbish MICE/Mu2e cryostat at Fermilab

## Slide 19: High Field Solenoids added to MDP
US Magnet Development Program recognized the need for high field solenoid R&D – added Area II: High Field Solenoids for HEP
“This is a new Area within MDP, and the goal is to leverage synergies with the NHMFL and Fusion applications to rapidly develop solenoid technologies tailored to HEP needs.”

## Slide 20: Concluding Remarks
HTS very promising for Muon Collider Magnets, but still a considerable amount of R&D required
  Conductor fabrication/characterization, magnet design, winding techniques, splice/ joint methods, mechanical structure, quench protection, cooling schemes….!
  Interest from Fusion driving down cost
Muon collider magnet designs maturing
  Iteration needed between HTS R&D and lattice
  Number of 6D cooling solenoid types should be reduced
Facility needed for testing larger/coupled coils